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JABÓN BASE MANTECA DE KARITE

Appearance at 25°C - Solid, opaque
Color: White / Ivory white
Water content, % - 25-30
Sodium Chloride content, % - 0.7-0.9
pH value (2% water solution) – 9.5-10.5
Melting temperature, °C – 60-65
Storage conditions: Store in a cool, well ventilated area away from direct sunlight and
moisture.
Ingredients (INCI): Aqua, Glycerin, Propylene Glycol, Sodium Laureth Sulfate, Sodium Stearate, Sorbitol, Sodium Laurate, Sodium Chloride, Butyrospermum Parkii (Shea Butter)*, Polysorbate 20, Sodium Thiosulfate, Titanium Dioxide, Etidronic Acid.
*Organic Certified
Melting procedure: the soap base is best melted in a double boiler, but can be melted in the microwave. Heating the base more than 70°C may cause the soap to dehydrate, reduce lather, and turn yellow. Add the colorants, oils or other ingredients. Pour the soap into the mould, allow time for the soap to set into the moulds shape, once set, remove from mould.
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